## Slide 1: Status of CCD Vertex Detector R&D for GLC
Yasuhiro Sugimoto
KEK
KEK/Niigata/Tohoku/Toyama Collaboration
@ACFA WS,Mumbai, Dec. 16, 2003

## Slide 2: Outline
Introduction
R&D for thin wafer
Study of radiation tolerance
  Expected beam background
  Electron damage study -- H.E. beam/beta ray
Study of charge spread
Possible design of Vertex Detector for GLC
Summary and outlook

## Slide 3: GLC Detector

## Slide 4: GLC Detector
 | Baseline Design | Possible Option
Vertex Detector | CCD | MT-CCD or CMOS
Intermediate Tracker | Silicon Strip Det. | 
Central Tracker | Jet Chamber | TPC
Solenoid Field | 3T | 4T
Calorimeter | Pb/Sci (Tile-Fiber) | Digital Cal.
Beam X’ing Angle | 7 mrad | 20 mrad

## Slide 5: Introduction
To get the excellent vertex resolution
  High spatial resolution of the sensor
  Thin material to minimize the multiple scattering
  Put the detector as close to the IP as possible
     Radiation tolerance
CCD
  1.  Excellent resolution by charge sharing :  < 3 m
  2.  Sensitive layer ~20 m, Mechanical Strength?
  3.  Not clear. Need R&D.
  Other R&D item : Readout Speed
  CCD: simple structure  Large size wafer with high yield

## Slide 6: R&D for thin wafer
Structure of CCD
  p+ substrate : ~300m
  Epitaxial p layer : ~20m
  n layer : few m
   We need only ~20m for
  charged particle detection

## Slide 7: R&D for thin wafer
How to support thin wafer?
  Backing
  Stretching
  Partial thinning
    Large area thinning brings non-flatness
    Ordered several wafers with different cell sizes
    Aim average thickness < 100m

## Slide 8: Study of radiation tolerance
Expected Beam Background at GLC
  Neutron : Mainly from downstream of the beamline 108~109 /cm2y (depends on beam line design)
  Electron/Positron : Pair background through beam-beam interaction -- Strongly depends on B and R
 | B=3T, R=24mm | B=3T, R=15mm | B=4T, R=15mm
Hits/train ( /mm2) | 0.3 | 2 | 1
Hits/y (107sec) ( /cm2) | 0.5x1011 | 3x1011 | 1.5x1011

## Slide 9: Study of radiation tolerance
Damage in CCDs
  Surface Damage
    dE/dx in SiO2 
      Surface dark current
      Flat-band voltage shift
  Bulk Damage
    Lattice dislocation in Si bulk 
      Bulk dark current
      Charge transfer inefficiency (CTI)  Trap Levels

## Slide 10: Study of radiation tolerance
NIEL Hypothesis
  Bulk damage is thought to be proportional to non-ionizing energy loss (NIEL)
  NIEL of electrons has strong energy dependence
  e+/e- pair background hitting the inner-most layer of VTX at LC peaks at ~20MeV
   High energy electron beam irradiation test
  NIEL of neutrons is ~x10 than that of H.E. electrons, but expected b.g. rate is 1/100~1/1000
   Not so serious

## Slide 11: Study of radiation tolerance
Sr-90
GLC b.g.

## Slide 12: Electron Damage Study
Test Sample CCDs
  256x256 pixels
  Made by Hamamatsu
  Readout Freq : 250kHz
  Readout Cycle : 2 sec
  Irradiation:
    At room temperature
    Without bias/clock
    Sr-90: 0.6, 1.0, 2.0 x 1011/cm2
    150 MeV beam: 0.5, 1.0, 2.0, 5.0 x 1011/cm2

## Slide 13: Electron Damage Study
Measurement of CCD characteristics
  Dark current
  Spurious dark current
  Flat-band voltage shift
  Charge transfer inefficiency (CTI)

## Slide 14: Electron Damage Study
Hot Pixels
  Observed only in beam-irradiated CCDs
  Presumably due to cluster defects which cannot be created by low energy electrons
Sr-90
1x1011/cm2
2x1011/cm2
150MeV Beam
Before Irradiation
1x1011/cm2
Measured at +10 C, Cycle time: 2 sec

## Slide 15: Electron Damage Study
Charge Transfer Inefficiency (CTI)
  Derived from position dependence of Fe-55 X-ray(5.9keV) peak
  CTI induced by 150MeV beam is x2~3 larger than Sr-90 induced CTI
  CTI suppression by fat-zero charge injection was observed
Beam
Sr-90

## Slide 16: Electron Damage Study

## Slide 17: Electron Damage Study

## Slide 18: Electron Damage Study
CTI improvements
  Notch channel : 1/3
  Fat-zero charge injection
  Fast readout speed
  Wide vertical clock
  Reduction of # of transfer
   Multi-port CCD

## Slide 19: Study of charge spread in CCD
Diffusion of electrons in epitaxial layer
  Key of excellent spatial resolution for CCD ( and CMOS )
  Takes time to diffuse :
  How long do we have to wait for the charge collection ?
   Measurement with
  IR LASER pulse

## Slide 20: Possible design of the CCD vertex detector for GLC
Standard CCD
  >>100MHz speed is needed for 6.3ms readout
Multi-port CCD
  Wide vertical clock cannot be used
Multi-thread CCD
  Optimum in terms of radiation tolerance
  R&D necessary

## Slide 21: Possible design of the CCD vertex detector for GLC
Baseline design
  R=24, 36, 48, 60 mm
  |cos| < 0.9
   = 4 m
  Wafer thickness = 300 m
  B = 3T
   b = 7  20/(psin3/2m
R&D milestone
  R=15, 24, 36, 48, 60 mm
  |cos| < 0.9
   = 4 m
  Wafer thickness = 100 m
  B = 4T
   b = 5  10/(psin3/2m

## Slide 22: Possible design of the CCD vertex detector for GLC
Expected signal loss by CTI
  Assume 32(V)x2000(H) pixels at R=15mm, B=4T
  Measured CTI: 3x10-4 (V), <5x10-5 (H) for 1x1011e/cm2 @-70 C w/o fat-zero charge injection
  Simulated pair b.g. in 1 year (107s): 1.5x1011e/cm2
   Signal loss: 1.5% (V), < 15% (H)
  With notch channel: 0.5% (V), < 5% (H)
  Fat-zero charge injection, wider V-clock, faster H-clock will improve the CTI still more
  Even room temperature operation might be possible

## Slide 23: Summary and outlook
R&D status for CCD vertex detector for GLC:
  Study of partially thinned wafer: Sample wafers ordered
  Radiation damage study: 150MeV beam irradiation test was carried out, and we found
    Hot pixel generation
    x2~3 larger CTI than 90Sr irradiated CCDs
    CTI suppression by fat-zero charge injection
  Charge spread in CCDs is being studied

## Slide 24: Summary and outlook (cont.)
Future plan
  Extend the present R&D :
    Optimize the design of partially thinned wafer
    CTI study as a function of clock width, speed, and amplitude
  Study the feasibility of Multi-thread CCD and try to make the prototype CCD + readout ASIC