## Slide 1: FPCCD Vertex Detector for ILC
2007.2.6
@9th-ACFA, Beijing
Y. Sugimoto
KEK

## Slide 2: Challenge of ILC VTX
Pair background at small R
  ~2000 tracks/cm2/train with B=3T and R=20mm
  Pixel occupancy ~10% for 25m pixel, if the signal of one bunch-train (2820 bunches) is accumulated
  In order to keep the occupancy small (<1%),
    read out 20 times per train (1ms), or
    20 times finer pixel
  is necessary
Track density (/cm2/BX)
To achieve the performance goal of IP = 5 10/(psin3/2) m;
  Material budget should be small: < 0.1% X0 / layer
  1st layer should be put as close to the IP as possible
 FPCCD
Electro-magnetic interference (EMI) caused by short-bunch beam

## Slide 3: FPCCD Vertex Detector
Accumulate hit signals for one train (2840 BX) and read out between trains (200ms)  Completely free from EMI
Fine pixel of ~5m (x20 more pixels than “standard” pixels) to keep low pixel occupancy
  Spatial resolution of ~1.5m even with digital readout
  Excellent two-track separation capability
Fully depleted epitaxial layer to minimize the number of hit pixels due to charge spread by diffusion
Two layers in proximity make a doublet (super layer) to minimize the wrong-tracking probability due to multiple scattering
Three doublets (6 CCD layers) make the detector (in GLD DOD)
Tracking capability with single layer using hit cluster shape can help background rejection
Multi-port readout with moderate (~20MHz) speed (Very fast readout (>50MHz) not necessary)
Simpler structure than FAPS or ISIS  Large area
No heat source in the image area

## Slide 4
Standard CCD
Fine Pixel CCD
 | High Pt Signal | 
 |  | Low Pt b.g.
Z  |  | 
B.G. rejection by hit cluster shape
(tracking capability with single layer!)
 B.G. suppression factor of 2 (cos~0) – 20 (cos~0.9) is expected

## Slide 5
Layer | R (mm)
1 | 20
2 | 22
3 | 32
4 | 34
5 | 48
6 | 50

## Slide 6: Challenge of FPCCD
Fully depleted – charge spread
Lorentz angle
  tan=rHB, rH: Hall coefficient~1, : mobility (m2/Vs), B: Magnetic field (T)
  Stronger E-field in dep. layer (>104V/cm = 1V/m) gives saturation of carrier velocity and smaller 
   Epi layer of ~15m would be OK
Radiation tolerance
Small pixel （~5 m)
Fast readout speed（~20Mpix/s）
Multi-port readout
  H-Register in image area
Low noise:
  <50 e (total)  < 30 e (CCD)
Low power consumption
  Metal layer
  Low drive pulse voltage
  Output circuit
Large area:10x65mm2（in）/20x100mm2（out）
Thin ladder （<0.1%X0/layer)
  Essential for FPCCD option (high hit density)
Full well capacity
  >104 e is OK
Readout ASIC
  Necessary for proto-type ladder

## Slide 7: Lorentz angle
tan=rHB~B (:m2/Vs, B:T), =v/E
~0.1 m2/Vs
~0.07 m2/Vs
~0.14 m2/Vs

## Slide 8: R&D for FPCCD
Study of fully depleted CCD
  Charge spread
  Lorentz angle
  Radiation damage
Development of FPCCD
  3 rounds expected
  Prototype ladder in 5 years
  Collaboration with Hamamatsu
Minimization of material budget
  Wafer thinning
  Si-RVC-Si sandwich structure
Development of readout ASIC
Partially funded

## Slide 9: Study of charge spread
Apparatus
CCD for reference
(Front-illumination)
CCD for test
(Back-illumination)

## Slide 11: Charge spread
Front illumination
Standard
Back illumination
Deep2 (30m epi)
Full-depletion
not complete
Try thinner epi

## Slide 12: FEA of Ladders
Si (CCD wafer)
RVC (Reticulated Vitreous Carbon)
10 cm
Epoxy
Deformation by self-weight is calculated by
FEA program COMSOL

## Slide 13: FEA of Ladders
Parameters (assumption)
Geometry
 | Density (g/cm3) | X0 (g/cm2) | E (GPa)
Si | 2.33 | 21.8 | 110
Epoxy | 1.15 | 40.9 | 3
RVC | 0.05 | 42.7 | 0.031
 | Thickness | Weight | Radiation length
Si | 50 m | 0.01165 g/cm2 | 0.0534%X0
Epoxy | 50 m | 0.00573 g/cm2 | 0.014%X0
RVC | 2 mm | 0.0084 g/cm2 | 0.0234%X0
Epoxy | 50 m | 0.00573 g/cm2 | 0.014%X0
Si | 50 m | 0.01165 g/cm2 | 0.0534%X0
Sum |  | 0.04316 g/cm2 | 0.1582%X0
0.08%X0/layer

## Slide 14: FEA of Ladders
Results
  Maximum deformation:
    Without gap : vmax=0.536 m
    With 0.2mm gap : vmax=0.723 m
  For longer ladders
    vmax ~ l4  ~8.6 m for 20cm ladder without gap

## Slide 15: Summary
We have started R&D of FPCCD for ILC vertex detector
Study of fully depleted CCD is on going in FY2006, and will be continued to FY2007
  CCD sample with 30m epi seems not fully depleted
  We will try to measure 15m epi sample soon
  Lorentz angle measurement and radiation damage test are planned
Finite element analysis was done for a ladder of Si-RVC-Si sandwich structure
  0.08% radiation length per layer with [50m Si]x2 + [50m epoxi]x2 + [2mm RVC]
  Deformation by self weight is less than 10m for 20cm long ladder
The 1st test sample of FPCCD is expected to be made by Hamamatsu in FY2007
We wish to construct and test prototype ladders of FPCCD in 4years, but the budget (for r.o. ASIC and support structure) is not enough to complete that goal