## Slide 1: R&D Status/Plan for FPCCD VTX Detector
2007/5/31
Y. Sugimoto
KEK
@LCWS2007

## Slide 2: FPCCD Vertex Detector
Accumulate hit signals for one train (2840 BX) and read out between trains (200ms)  Completely free from EMI
Fine pixel of ~5m (x20 more pixels than “standard” pixels) to keep low pixel occupancy
  Spatial resolution of ~1.5m even with digital readout
  Excellent two-track separation capability
Fully depleted epitaxial layer to minimize the number of hit pixels due to charge spread by diffusion
Two layers in proximity make a doublet (super layer) to minimize the wrong-tracking probability due to multiple scattering
Three doublets (6 CCD layers) make the detector (in GLD DOD)
Tracking capability with single layer using hit cluster shape can help background rejection
Multi-port readout with moderate (~10MHz) speed (Very fast readout (>50MHz) not necessary)
Simple structure  Large area
No heat source in the image area

## Slide 3
Layer | R (mm)
1 | 20 (18)
2 | 22 (20)
3 | 32
4 | 34
5 | 48
6 | 50

## Slide 4: Development of Fully-depleted CCD by HPK
Confirmation of full-depletion using line-focused LASER
  LASER light (532nm) focused to a thin (<pixel size) line was illuminated to CCDs slightly inclined w.r.t. CCD pixel grid Effectively scan inside a pixel
  Compare signal distribution between Vgate=-7V and Vgate=+6V during LASER illumination
  If distributions are same, the CCD is fully depleted in both cases
Laser

## Slide 6: Potential v.s. Vgate
Vgate=0 – 6 V

## Slide 7: Results
Projection

## Slide 8: S7170 Standard
Back-illumination
Low resistivity epitaxial layer  thin depletion layer
S.N.; BF3-006
-7V
+6V
1 pixel

## Slide 9: S7170 Deep2
Higher resistivity 30m thick epitaxial layer
SN; FF16-011
-7V
+6V

## Slide 10: S7170 SPL 15m
Higher resistivity 15m thick epi-layer
SN;11-12
-7V
+6V

## Slide 11: S7170 SPL 24m
Highest resistivity 24m thick epi-layer
SN; 22-20
-7V
+6V

## Slide 12: Conclusion
Fully depleted epitaxial layer is the key issue of FPCCD vertex detector
The signal distributions of a newly developed CCD, S7170-0909 SPL 24m, at two different gate voltages of -7V and +6V during the LASER illumination were same
From this result, we can conclude that S7170-0909 SPL 24m is fully depleted even at the gate voltage of -7V
Measurement of Lorentz angle and study of radiation hardness of this CCD are planned in this FY
Fabrication of smaller pixel, multi-port readout CCD and ASIC for readout of the multi-port CCD are also planned in this FY